[image: image1.png]M AT s u I 1501 West 178th Street | Gardena, California 90248

INTERNATIONAL COMPANY, INC.  310-767-7812 | 800-359-5679 | fax: 310-767-7836 | info@matsui-color.com | www.matsui-color.com




AQUALITE COLORING SYSTEM

Chromicolor® AQ Ink / Photopia® AQ Ink 
GENERAL INFORMATION

This product is a water based Chromicolor® or Photopia® paste with clear dilutant and thinners, specifically formulated to be used in the Aqualite Coloring System pigment dyeing process for cotton products.
COLOR INFORMATION

Chromicolor®
Chromicolor® changes color with temperature.  The darker color (Chromicolor®) is seen when cold and the color disappears (or changes to a lighter color) when heated.  There are eleven standard colors in Chromicolor® as follows:
	New Fast yellow
	Pink
	Brilliant Green

	Gold Orange
	Magenta
	Fast Black

	Vermilion
	Fast Blue
	Green

	
	Turquoise Blue
	Brown


To achieve a color to color effect, a water base pigment can be mixed with the Chromicolor® in the dyeing process.  
Photopia®
Photopia® comes in three basic colors:  Colorless to Purple, Colorless to Yellow and Light yellow to Blue.  The colors “appear” in the sunlight or with UV light.  You can achieve a color to color effect by mixing a conventional pigment into the AQ ink.

(Photopia® changes at 340 – 370 nanometers)

PRODUCT SPECIFICATIONS

	Solids, Theoretical:
	Chromicolor® AQ Ink 
	33%

	
	Photopia® AQ Ink
	33%

	
	
	

	Coverage, theoretical:
	35g/meter + 2.5g,
	

	
	Based on a 120 mesh screen
	

	
	
	

	Viscosity, as shipped:
	Chromicolor® AQ Ink
	8,000-10,000cps @ 25 C

	BH Model Viscometer
	Photopia® AQ Ink
	8,000-10,000cps @ 25 C

	
	
	

	Specific Gravity:
	Chromicolor® AQ Ink – 
	1.05

	
	Photopia® AQ Ink -        
	1.02

	
	
	

	Flash Point:
	Chromicolor® AQ Ink
	Non-combustible

	
	Photopia® AQ Ink
	Non-combustible


	MATERIALS
	AMT. TO BE USED
	DESCRIPTION

	Fixer P-1
	6% owf
	Pre-treatment agent

	Matsuminsol MR-50
	10-15% owf
	Adhesive

	Chromicolor® AQ Ink
	10-20% owf
	Temperature sensitive colorant

	Photopia® AQ Ink
	10-20% owf
	Light sensitive colorant

	PG Color MI
	0-2% owf
	General pigment (to achieve color to color change)

	Glow Color MI
	0 – 5% owf
	Fluorescent pigment (to achieve color to color change)


PROCESSING METHOD
Process using Rotary Drum dyeing machine or Smith Drum dyeing machine.

•  Perform scouring / bleaching to fabric as needed 

•  Drain and add fresh water in ratio of 1:20-35 
•  Add 6% owf Fixer P-1 to machine

•  Raise temperature to 70°C (158°F).  Keep temperature at 70°C for 15 minutes

•  Drain and rinse well with cold water (about 3 minutes).  Repeat if needed.

•  Drain and add fresh water in ratio of 1:15-20 and raise the temperature to 70°C
•  Add 15-20% owf Chromicolor® / Photopia® AQ Ink.  If color to color effect is desired up to 2% PG pigment or 5% Glow color can be added.
•  Keep 70°C for 15 minutes
•  Add 10-15% owf of Matsuminsol MR-50 to the AQ Ink bath.  Keep 70°C for 5-10 minutes.
• Drain and rinse with cold water for about 2 minutes.  Repeat as needed.  Perform softening treatment if desired.  Spin dry.

•  Dyeing machine can be cleaned using Highclean AQ-2.
SHELF LIFE, STORAGE, SAFETY, HANDLING


Shelf life:
Shelf life of unmixed ink is 6 months at a






temperature of 30 C.  Reducing the storage






temperature to 10 C extends the shelf life to six






months minimum.


Storage:
Protective clothing should be worn at all times when using
Lead time:
Some colors/types are kept in stock.  Stock goods can ship within a day or two of order.  If goods need to be produced then lead time is about 3 ½ - 4 weeks, plus shipping from Japan.


Chromicolor® and Photopia® Aqualite Coloring System
Page 2 of 2

